# Ultrasonic Testing Report

| Report No. NIIT/WIL/UT/278 Page No: 1 /1 |  |  |  | Job Description: 783107 HS200 NOZZLE END SEGMENT [HS200-NES-20-WIL] |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Report Date: 26.07.2025 |  |  |  | Weld Joint No.: As per Annexure I |  |  |  |  |  |  |  | Thickness of Job: 7.8MM / 7.7MM / 12MM / 18MM |  |  |  |  |  |  |
| Surface Condition: Ground and polished |  |  |  | Customer: M/s WIL, Walchandnagar |  |  |  |  |  |  |  | Period of Inspection: 21/07/2025 To 24/07/2025 |  |  |  |  |  |  |
| Material: MDN 250 |  |  |  | Scanning technique: Contact manual |  |  |  |  |  |  |  | Stage of Inspection: Before HT / AA Periodic UT / After Ageing / After PPT |  |  |  |  |  |  |
| Equipment Used: USM-36 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Couplant: Oil+ Grease |  |  |  | Area scanned: Weld + HAZ (Longitudinal & Transverse – 2 Directions) |  |  |  |  |  |  |  | Acceptance Standard: MME/QC-HTW/M250/001 REV.0 / CUSTOM |  |  |  |  |  |  |
| Reference datum: RT Location |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Test Setup For Angle Range:0-100 mm For Normal Range:0-10 mm |  |  |  | Standard Cal Block: For Angle: V-2 Block (MDN-250) For Normal: Step Block (MDN 250) |  |  |  |  |  |  |  | Idtn. No of Ref Block: For Angle ‘G’ Notch (LSP 34 A side only) For Normal 2mmFBH (PJS-01-2007/4) / CUSTOM |  |  |  |  |  |  |
| Angle Probe calibration |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Frequency: 4 MHZ |  |  |  | Size: 8x9 mm |  |  |  |  |  |  |  | Type: MWB |  |  |  |  |  |  |
| Sr. Nos. of probes | 45 - 63230 |  |  |  |  |  |  | 60 - 63285 |  |  |  |  |  | 70 – 63309 |  |  |  |  |
| Scanning | 45 L |  |  |  | 45 T |  |  | 60 L |  |  | 60 T |  |  | 70 L |  |  | 70 T |  |
| Skips | BP mm |  | %FSH |  | BP mm | %FSH |  | BP mm |  | %FSH | BP mm | %FSH |  | BP Mm |  | %FSH | BP Mm | %FSH |
| ½ | 09 |  | 80 |  | 10 | 80 |  | 12 |  | 80 | 12 | 80 |  | 14 |  | 80 | 14 | 80 |
| 1 | 19 |  | 80 |  | 20 | 66 |  | 24 |  | 82 | 24 | 60 |  | 28 |  | 85 | 28 | 55 |
| 1½ | 29 |  | 46 |  | 30 | 32 |  | 36 |  | 76 | 36 | 26 |  | 41 |  | 70 | 42 | 22 |
| 2 | 39 |  | 75 |  | 40 | 25 |  | 47 |  | 80 | 48 | 20 |  | 55 |  | 82 | 56 | 10 |
| DAC dB | 46.0 dB |  |  |  | 44.0 dB |  |  | 48.5 dB |  |  | 50.0 dB |  |  | 52.5 dB |  |  | 54.0 dB |  |
| Scanning dB | 46.0 + 10dB |  |  |  | 44.0 + 10dB |  |  | 48.5 + 10dB |  |  | 50.0 + 10dB |  |  | 52.5 + 10dB |  |  | 54.0 + 10dB |  |
| Normal Probe calibration |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Probe S. No/Type: |  | 75798 / MSEB 4E |  |  |  |  |  |  | Frequency:4 MHz |  |  |  |  |  | Size: 10 mm (TR) |  |  |  |
| Skip |  | 4.0 BP – 80 % |  |  |  |  |  |  | DAC dB = 49.0 dB |  |  |  |  |  | Scanning dB = 49.0 + 10 dB |  |  |  |
| Disposition: ACCEPTED / NOT ACCEPTED |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Remarks (If any): RECORDABLE INDICATIONS WAS OBSERVED - REFER ANNEXURE– I / NO RECORDABLE INDICATIONS WAS OBSERVED / CUSTOM |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| National Ind. Insp. & Training |  |  |  |  |  |  | QC/WIL |  |  |  |  |  | RQS/VSSC |  |  |  |  |  |
| Signature: |  |  |  |  |  |  | Signature: |  |  |  |  |  | Signature: |  |  |  |  |  |
| Name: Mr. Ejaj Patel |  |  |  |  |  |  | Name: |  |  |  |  |  | Name: |  |  |  |  |  |
| Date: 26.07.2025 |  |  |  |  |  |  | Date: |  |  |  |  |  | Date: |  |  |  |  |  |